MTI supplies all kinds of high quality fluoride single crystals. These crystals have been widely used for infrared optical components, such as window, mirror, lens, prism and substrate. MTI has a state of art processing facility in China and provides you cost effective and high quality components.

| Chemical formula | BaF2 | CaF2 | MgF2 | LiF |
| --- | --- | --- | --- | --- |
| Crystal structure | Cubic | Cubic | Tetragonal | Cubic |
| Lattice constant (Å ) | 6.196 | 5.462 | a = 4.64 c = 3.06 | 4.026 |
| Melting point ( oC ) | 1354 | 1418 | 1255 | 870 |
| Density ( g / cm3 ) | 4.88 | 3.18 | 3.18 | 2.60 |
| Hardness | 3 | 4 | 6 | 4 |
| Thermal expansion coef. ( oC-1x 10-6 ) | 18.1 | 18.85 | 13.7 | 37.0 |
| Refractive index | ho 1.47443 | ho 1.43382 | ho 1.37740 he 1.38945 | ho 1.39212 |
| Transmission waveband (microns) | 0.15 - 13.00 | 0.11 - 12.00 | 0.11 - 7.5 | 0.11 - 7.0 |
| Transmission efficient | > 93% @ 5 m > 75% @ 0.2 m | > 94% @ 5 m > 85% @ 0.2 m | > 93% @5 m > 85% @ 0.2 m | > 85% @ 5 m > 65% @ 0.2 m |
| Chromatic dispersion (hf-hc) | 0.00578 | 0.00455 | 0.00355 | 0.00395 |
| Temperature coef. (dh/dt x 10-6 ) | -15.2 ~ 6.2@ 0.8 m | -10. 6 @ 0.8 m | 2.3 ~1.7 @ 0.4 m | -12.7 @ 0.6 m |
| Crystal growth method | Bridgeman | Bridgeman | Bridgeman | Bridgeman |
| Cleavage plane | <111> | <111> | <100> or <110> | <100> |
| Max. Crystal size ( mm) | f 2" x 80 | f 8" x 150 | f 4" x 100 | f 4" x 80 |
| Application | IR and UV window , prism, substrate | IR window and Lens, prism | VUV window and mirror, lens | UV window and prism, without deliquescence |

If you have any need for fluoride single crystal substrate and components, please feel free to contact us at

info@mtixtl.com

Please kindly specify your crystal size, faces to be polished and orientation, and quantity; we will reply you within 24 hours